## Slide 1
Bipyramids + Ag – Série CGCH-158C
0,2 eq
0,6 eq
0,8 eq
0,4 eq
1 eq
4 eq
8 eq
2 eq
CGCH-158C1
CGCH-158C3
CGCH-158C4
CGCH-158C2
CGCH-158C5
CGCH-158C7
CGCH-158C8
CGCH-158C6
Rajouter BPs initiales
CGCH-158C
Au@Ag nanorods ar made from a purified sample of bipyramids. Their cross section is pentatwinned.
Here I added increasing quantitied of silver, from 0,2 to 8 eq. The width will be almost constant and the length will increase.
There can be some impurities due to aggregation of bipyramids, or inhomogeneous deposition of silver on the bipyramids.

## Slide 2
Chart: Wavelength (nm)
0,2 eq
0,6 eq
0,8 eq
0,4 eq
1 eq
4 eq
8 eq
2 eq
Initial BPs
More Ag